# TECHNICAL DATA SHEET

021 Series

PRO-PREP COMPLETE

One Coat Coverage

Drywall Primer

Specially formulated for the Florida climate

__________________________________________________________________________________________

Povia 021 PRO-PREP COMPLETE  is a pigmented sealer designed to prime and seal new drywall surfaces which allows for uniform application of the finish coat.

__________________________________________________________________________________________

RECOMMENDED USES:

For application to uncoated drywall or similar composition wallboard.  Apply as a barrier coat to insure uniformity of the finish coat..

SURFACE PREPARATION:

Dirt, grease, grime and any foreign material must be removed before application of new coating.  Treat surface for mildew.  Be sure surface is clean and dry.

APPLICATION INFORMATION:

Mix product thoroughly and apply with brush, roller or airless sprayer.  When spraying, use a tip designed for flat wall coatings.  Apply when surface and air temperatures are above 50 Deg. F.

RECOMMENDED THINNER:

Povia 021 does not require thinning and should be used as is, directly from the container.

TECHNICAL DATA:

Finish: Flat

Pigment Type: Titanium Dioxide & Inert Pigments

Vehicle Type: Acrylic Copolymer

Solvent Type: Water

% Solids By Weight: 52% +/- 2%

% Solids By Volume: 34% +/- 2%

Density: 11.45 lbs. Per gallon

Viscosity @ 75 deg. F (24 deg. C): 100 +/- 2 K.U.

Coating VOC: <100 g/l

Estimated Dry Time:  To touch 30-60 minutes ; Recoat 4-6 hours

Flash Point, Minimum: Not Flammable

Flame Spread: Class A rating on non-combustible substratum

Recommended Dry Film Thickness Per Coat: 1.0-2.0 Mils DFT.

Clean Up: Clean up drips and spills immediately using a damp cloth.  Clean tools and equipment with soap and fresh water.

Coverage (Theoretical): Coverage will depend on porosity and contour of the surface being coated.    Coverage typically averages 200-300 square feet per gallon.

Povia 021  is water based.  Do not Freeze.

CAUTION: KEEP OUT OF REACH OF CHILDREN!

WARNING! If you scrape, sand or remove old paint, you may release lead dust.  LEAD IS TOXIC.  EXPOSURE CAN CAUSE SERIOUS ILLNESS, SUCH AS BRAIN DAMAGE, ESPECIALLY IN CHILDREN.  PREGNANT WOMEN SHOULD ALSO AVOID EXPOSURE.  Wear an NIOSH-approved respirator to control lead exposure.  Carefully clean up with a HEPA vacuum and a wet mop.  Before you start, find out how to protect yourself and your family by contacting the National Lead Information Hotline at 1-800-424-LEAD or log on to www.epa.gov/lead.

Technical data contained herein is true and accurate at the date of issue, but is subject to change without notice.  A Povia Paints representative should be contacted with any questions concerning product information or application procedures.  Our products conform to Povia quality standards, but no other warranty is expressed or implied.  Liability, if any, is limited to the replacement of product or purchase price.

## Povia Paints, Inc., 5601 Banner Dr., Ft. Myers, FL 33912  239-791-0011

www.poviapaints.com